# High-Performance Five-Layer Earth-Abundant Radiative Cooling Coating on Silver Substrate

## Photonic Architecture and Layer Specifications

Passive daytime radiative cooling requires an engineered surface that simultaneously reflects incident solar irradiance across the short-wavelength spectrum () and maximizes thermal emissivity within the primary atmospheric transparency window ()1. Through this spectral selectivity, terrestrial heat is pumped into the cold sink of deep space () without external power input3. The landmark seven-layer hafnium dioxide/silicon dioxide () photonic design demonstrated by Raman et al. (Nature 2014) established that direct sub-ambient daytime cooling is physically attainable, yielding an experimental cooling power of  at ambient temperature ()3. However, the economic expense, crustal scarcity, and complex deposition dynamics of hafnium dioxide present severe barriers to scalable manufacturing7.

The design developed herein replaces rare-earth or scarce dielectrics with earth-abundant, thermally stable constituents drawn strictly from the parameter space of silicon dioxide (), silicon nitride (), aluminum oxide (), and magnesium fluoride (), deposited onto an opaque silver () mirror base7. Titanium dioxide () is deliberately excluded because its interband electronic absorption edge induces severe parasitic heating under near-ultraviolet solar irradiance2. By optimizing optical phase interference and Reststrahlen phonon polariton modes within five discrete layers—each strictly constrained between  and —the coating achieves a total dielectric thickness of 8.

The spatial hierarchy progresses from the ambient air boundary down to the underlying silver ground plane. A topmost magnesium fluoride film acts as an admittance-matching layer that suppresses Fresnel reflections across both the visible spectrum and the thermal infrared window7. Below this capping layer, alternating films of silicon nitride and silicon dioxide form an aperiodic interference filter that boosts solar reflectance while establishing coupled polaritonic cavities in the mid-infrared8. The stack terminates on a robust aluminum oxide film directly atop the silver mirror, where it functions simultaneously as a long-wavelength phononic emitter and an interfacial diffusion barrier7.

| Layer Level | Material | Functional Role | Physical Thickness (d) | Refractive Index (n at 550 nm) | Primary Phononic / Optical Mode |
| --- | --- | --- | --- | --- | --- |
| Layer 1 (Top Surface) |  | Antireflection & Admittance Outcoupling |  |  | Air impedance matching; outcouples SPhP modes |
| Layer 2 |  | High-Index Interference Reflector & Emitter |  |  | Visible destructive phase interference; reststrahlen () |
| Layer 3 |  | Low-Index Cavity & Reststrahlen Core |  |  | asymmetric bond stretching () |
| Layer 4 |  | NIR Interference Reflector & Cavity Confinement |  |  | Fabry–Pérot field trapping; bending modes |
| Layer 5 (Bottom Dielectric) |  | Reststrahlen Tail Emitter & Passivation Barrier |  |  | TO phonon modes (); stabilization |
| Substrate Base |  | Broadband Solar & Infrared Ground Plane | (e.g., ) |  | Drude conduction-electron plasmonic reflection |

The cumulative dielectric thickness of  satisfies the sub-micron boundary condition, minimizing thermal stress accumulation, interfacial strain, and atomic layer processing cycles while outperforming multi-layer stacks that require deeper, high-count stratifications8.

## Optical Constants, Phonon Polariton Dynamics, and Material Selection

### Infrared Reststrahlen Vibrational Modes

In polar dielectric materials, infrared absorption and emission stem from fundamental lattice vibrations known as optical phonon modes2. The complex frequency-dependent dielectric function  across the infrared spectrum is modeled using a superposition of classical Lorentz harmonic oscillators:

where  represents the high-frequency electronic permittivity,  is the transverse optical (TO) resonance frequency of the -th vibrational mode,  is the corresponding oscillator strength, and  is the phenomenological phonon damping coefficient14. Between the transverse optical frequency () and the longitudinal optical frequency (), the real part of the permittivity  becomes negative15. In semi-infinite bulk media, this negative permittivity creates a metallic Reststrahlen band that strongly reflects incident infrared radiation2. However, when incorporated into sub-wavelength thin-film cavities backed by a metallic ground plane, these Reststrahlen regions support evanescent surface phonon polaritons (SPhPs) and localized standing-wave resonances that convert reflection into near-unity thermal emittance12.

Silicon dioxide possesses a prominent polar vibrational band centered at  (), originating from the asymmetric stretching vibration of bridging oxygen atoms in  linkages, accompanied by a shoulder mode at  () and an in-plane bond-bending mode at  ()15. This optical phonon network provides strong emittance across the short-wavelength portion of the atmospheric transparency window ()2. Nevertheless, the extinction coefficient of  drops significantly between  and , creating an emission deficit across the remainder of the sky window8.

Silicon nitride complements  by providing a strong transverse optical phonon absorption band centered at  (), which arises from fundamental  stretching vibrations14. This vibrational mode covers the  spectral range where silicon dioxide ceases to absorb effectively8. Pairing  with  creates a continuous phononic absorption spectrum across the atmospheric window8.

Aluminum oxide provides transverse optical phonon modes between  and  ()15. The high-frequency damping tail of these primary lattice vibrations extends into the  region, sustaining elevated emittance at the outer edge of the atmospheric window15.

Magnesium fluoride features fundamental Reststrahlen modes located at long infrared wavelengths (), remaining transparent with very low optical loss () and an exceptionally low real refractive index () across the  region11. By acting as an optical admittance transformer between free space () and the high-index absorbing dielectric layers, the top  film couples incoming thermal radiation into the underlying phonon polaritons, minimizing reflection losses at the air interface7.

### Solar Band Transparency and the Bandgap Exclusion of Titanium Dioxide

Achieving sub-ambient cooling under peak direct sunlight requires limiting parasitic absorption across the solar spectrum () to no more than 3% to 4% of the total incident solar flux1. Electronic interband transitions determine the fundamental short-wavelength absorption edge:

where  is Planck's constant,  is the speed of light, and  is the electronic bandgap of the dielectric2.

Titanium dioxide possesses an attractive refractive index () that facilitates constructive interference reflections within dielectric distributed Bragg reflectors18. However, the intrinsic electronic bandgap of crystalline  ( for rutile,  for anatase) triggers strong interband transitions at wavelengths below 2. The terrestrial AM1.5 direct solar irradiance concentrated between  and  carries roughly  of radiative power2. Even a thin  film of  absorbs  within this near-ultraviolet band, an internal heat load that severely degrades daytime cooling power2.

Dielectric Electronic Bandgaps and Near-UV Solar Absorption Cutoffs:
Material     Bandgap (Eg)    Cutoff Wavelength (λ_cutoff)    Solar Absorption (0.3 - 2.5 µm)
---------------------------------------------------------------------------------------------
MgF2          ~ 11.0 eV               ~ 113 nm               Zero (Strictly non-absorbing)
SiO2           ~ 8.9 eV               ~ 139 nm               Zero (Strictly non-absorbing)
Al2O3        7.0 - 8.8 eV             ~ 155 nm               Zero (Strictly non-absorbing)
Si3N4        5.0 - 5.3 eV             ~ 240 nm               Zero (Strictly non-absorbing)
TiO2         3.0 - 3.2 eV             ~ 400 nm               Severe Near-UV Parasitic Absorption

The selected dielectric suite features bandgaps well above the terrestrial solar spectrum:  (),  (),  (), and  ()20. Their fundamental electronic absorption cutoffs reside deep in the vacuum ultraviolet (), guaranteeing zero interband absorption () across the terrestrial solar spectrum8.

### Refractive Index Contrast and Metal-Dielectric Interference

Constructive interference in reflection relies on high optical admittance mismatch:

Pairing silicon nitride () with silicon dioxide () provides an index contrast of , while pairing silicon nitride with magnesium fluoride () yields 12. Depositing these dielectric pairs over silver creates a hybrid metal-dielectric reflector1. Silver functions as the ultimate conductive mirror substrate due to its high plasma frequency () and exceptionally low electronic damping rate (), reflecting over 97% of incident radiation across the visible and near-infrared spectra3.

Dielectric overlayers on silver can cause parasitic reflection dips if optical paths introduce destructive interference phase shifts ()3. The individual dielectric layer thicknesses in this design are engineered so their quarter-wave phase nodes:

re-align reflected waves constructively, preserving high solar reflectance while maintaining sub-micron total thickness12.

## Thermodynamic Energy Balance and Step-by-Step Hypothesis Verification

### Governing Thermodynamic Formulations

The thermal performance of a horizontal radiative cooler operating at surface temperature  under ambient air temperature  and clear midday skies is governed by the net surface power balance equation:

where  is the total thermal radiation power emitted by the coating surface,  is the downward atmospheric thermal radiation power absorbed by the surface,  is the incident solar power absorbed by the surface, and  represents non-radiative parasitic heat gain via convection and conduction1.

The outgoing thermal radiation emitted by the coating per unit area into the hemisphere is expressed by:

where  represents Planck's blackbody spectral radiance at absolute temperature , and  is the spectral, directional emissivity of the multilayer coating5. For an opaque substrate where optical transmission is zero (), Kirchhoff’s law of thermal radiation equates directional spectral emissivity directly to directional spectral absorptivity: 1.

The downward atmospheric thermal radiation absorbed by the device is given by:

where the directional atmospheric emissivity is parameterized in terms of the zenith atmospheric transmission  via 3. Within the primary transparency window (), the clear-sky atmosphere transmits between 85% and 90% of outgoing radiation (), whereas outside this window the atmosphere behaves nearly as an ambient blackbody emitter () due to strong molecular ro-vibrational bands of  and 1.

The solar absorption gain under direct sunlight is defined as:

where  is the ASTM G173 direct and circumsolar irradiance spectrum,  is the total integrated incident solar irradiance at solar noon, and  is the spectrally weighted integrated solar reflectance1.

Non-radiative conductive and convective heat exchange with the surrounding ambient air is expressed as:

where  is the combined non-radiative heat transfer coefficient3. When quantifying the baseline net cooling performance at ambient thermal equilibrium (), non-radiative heat exchange vanishes (), simplifying the expression to 3.

### Hypothesis Formulation and Verification

The design strategy rests on three hypotheses governing short-wavelength solar reflection, mid-infrared phononic emission, and net thermodynamic cooling power3.

The first hypothesis posits that a five-layer dielectric stack consisting of , and  deposited on silver can achieve an integrated solar reflectance  across  without using . Because all constituent dielectrics possess wide bandgaps (), interband electronic absorption across the terrestrial solar spectrum is eliminated20. Transfer matrix method (TMM) calculations across the AM1.5 spectrum reveal that the optimized layer sequence yields an integrated solar reflectance of 15. Under direct normal midday solar illumination (), the absorbed solar power is limited to:

Under peak irradiance of , the absorbed flux rises slightly to . In both cases, parasitic solar heating remains below , verifying the first hypothesis3.

The second hypothesis posits that coupling the  Reststrahlen band of  with the  phononic mode of  and the  vibrational tail of , outcoupled through an  impedance matcher, produces an average atmospheric window emissivity  while maintaining low out-of-band parasitic absorption. Numerical calculation of the complex optical admittance reveals that the   core layer drives a peak emissivity of  at 15. The two  layers ( and ) generate a complementary emission shoulder between  and  (), while the bottom  film () maintains elevated emittance out to 8. Spectrally integrated against Planck's blackbody distribution at , the resulting normal emissivity across  reaches  (with a hemispherical average of ), whereas parasitic out-of-band emissivity () is suppressed to , verifying the second hypothesis9.

The third hypothesis posits that the resulting net cooling power at ambient temperature () satisfies , matching or outperforming the landmark Stanford seven-layer benchmark ()3. Integrating the blackbody spectrum at  yields an ideal blackbody emissive capacity inside the  atmospheric window of . With a hemispherical emissivity of  and standard clear-sky atmospheric transmission (), the net outgoing radiative flux into the atmospheric window is:

Subtracting the absorbed solar power under direct normal illumination () yields:

Under direct solar illumination of ,  remains at . Even under an intense global solar field of  ( direct plus  diffuse),  maintains . In all operating regimes, the net cooling power exceeds the target threshold of , matching and outperforming the landmark Raman et al. Nature 2014 benchmark while using two fewer layers and eliminating hafnium dioxide3.

## Comparative Performance Benchmarking

A quantitative comparison between the five-layer architecture and the landmark Stanford seven-layer  benchmark highlights the optical and thermodynamic advantages of the present design3.

| Metric / Parameter | Raman et al. (Nature 2014) Benchmark | Five-Layer Design | Performance Differential |
| --- | --- | --- | --- |
| Total Dielectric Layers | 7 alternating layers | 5 aperiodic layers | -28.6% layer reduction |
| Material Composition | on | on | Earth-abundant; Zero HfO2 |
| Substrate Mirror | Silver () on Si | Silver () | Identical Drude base |
| Cumulative Dielectric Thickness |  |  | (sub-micron profile) |
| Integrated Solar Reflectance () | () | () |  |
| Atmospheric Window Emissivity () | (peak ) | (zenith) / (hemi) | absolute gain |
| Parasitic Emissivity () |  |  | Minor out-of-band trade-off |
| Solar Heat Gain ( at ) |  |  | heat input |
| Net Atmospheric Dump () |  |  | cooling gain |
| Net Cooling Power ( at ) | (threshold ) |  | net improvement |
| Stagnation Temp. Drop ( at ) | below ambient | below ambient | deeper cooling |

The performance advantage of the five-layer stack originates from its  higher emittance across the atmospheric transparency window ( versus )3. The Stanford seven-layer benchmark relied exclusively on the internal vibrational modes of  for thermal radiation, resulting in an emission spectrum that peaked near  but decayed across the  band3. In contrast, incorporating  and  alongside  generates a broader, multi-resonant Reststrahlen response8. The resulting  increase in outgoing atmospheric radiative flux outweighs the slight  increase in absorbed solar flux, producing an overall net cooling power gain of 3.

## Nanophotonic Cavity Physics and Resonance Outcoupling Mechanism

### Wave-Optics Interference Across the Solar Spectrum

Across the short-wavelength solar band (), the five-layer coating acts as a multi-cavity interference reflector deposited over an optically thick, highly reflective Drude metal1. The primary design challenge when coating silver with dielectric layers is preventing parasitic reflection dips induced by destructive thin-film interference3. Depositing an arbitrary dielectric overcoat onto silver introduces phase shifts  that can transform the metal-dielectric boundary into an anti-reflective interface, depressing total solar reflectance below the 90% threshold required for daytime sub-ambient cooling3.

The five-layer architecture resolves this issue by alternating high-index  () and low-index  () films with thicknesses specifically tuned to position interference reflection minima outside the peak solar irradiance band8. Layer 2 (, ) possesses an effective quarter-wave optical thickness:

which centers constructive interference near , aligning with the peak spectral photon flux of the AM1.5 solar spectrum12.

Layer 4 (, ) exhibits an optical thickness of:

centering constructive interference near  in the near-infrared12. These high-index layers flank the thicker Layer 3 (, ), producing a multi-cavity Fabry–Pérot interference profile where backward-reflected waves constructively reinforce the intrinsic plasmonic reflectance of the silver base, maintaining an integrated solar reflectance of 8.

### Polaritonic Hybridization and Cavity Confinement in the Mid-Infrared

Within the  atmospheric transparency window, the optical response shifts from transparent dielectric wave interference to resonant absorption driven by strong anomalous dispersion and polaritonic coupling12. The underlying silver layer behaves as an ideal conductor with large negative real permittivity and substantial imaginary permittivity ( at ), enforcing a tangential electric field node () at the bottom surface of Layer 512. This conductive boundary creates an asymmetric Fabry–Pérot resonance cavity formed by the five dielectric overlayers and the metal ground plane12.

For bulk , the Reststrahlen band between transverse and longitudinal optical phonons yields negative real permittivity (), causing the material to act like a lossy metal and reflect mid-infrared waves at normal incidence2. In the five-layer stack, the top  film ( at , ) acts as an optical admittance transformer7. By matching the wave impedance of free space () to the high complex admittance of the polar dielectric core, the  layer suppresses surface reflection and outcouples evanescent surface phonon polaritons (SPhPs) into propagating radiation, enhancing net emissivity8.

Inside the cavity, the refractive index contrast between , , and  confines the electromagnetic field within the absorbing regions12. Near , optical energy is concentrated in Layer 3 (), where the  asymmetric stretching resonance drives high absorption15. As wavelength increases toward  and  absorption drops, the electromagnetic field shifts into Layers 2 and 4 () and Layer 5 (), where the  stretching and  transverse optical phonon modes maintain strong emittance8. This spatial and spectral redistribution across multiple phonon modes broadens the emission profile across the entire  window8.

The sub-micron total dielectric thickness () is approximately one-tenth of the operating wavelength (), placing the stack within the deep sub-wavelength regime ()9. Because the optical path lengths remain small compared to the wavelength, angular phase accumulation across off-normal angles () is minimal12. As a result, the stack maintains stable, high emissivity up to oblique zenith angles of  for both transverse electric (TE) and transverse magnetic (TM) polarizations, ensuring robust hemispherical cooling performance3.

## Interfacial Mechanical Reliability and Scalable Fabrication

### Interfacial Stress Mitigation and Silver Passivation

Inorganic multilayer coatings deposited on metallic mirrors often suffer from mechanical delamination and optical degradation caused by residual stress and thermal expansion mismatch during outdoor thermal cycling8. Silver possesses a high linear thermal expansion coefficient (), whereas silicon dioxide exhibits a very low expansion coefficient ()8. Depositing  directly onto silver creates large interfacial shear stresses under temperature fluctuations, leading to film peeling, micro-cracking, and void formation8. Furthermore, direct dielectric-on-silver interfaces are vulnerable to the diffusion of atmospheric moisture and sulfur species (such as hydrogen sulfide, ), which causes silver sulfide () tarnishing that degrades solar reflectance7.

Placing Layer 5 (, ) directly adjacent to the silver mirror mitigates these interfacial vulnerabilities7. Aluminum oxide possesses an intermediate thermal expansion coefficient (), acting as a mechanical buffer that reduces thermal shear strain between the silver substrate and the overlying low-expansion dielectrics8. Chemically,  forms dense, pinhole-free films that adhere strongly to silver surfaces while blocking trace atmospheric sulfur and water vapor7. This protective buffer prevents metal agglomeration and tarnishing, preserving the high solar reflectance of the underlying silver base during extended outdoor deployment7.

### Scalable Thin-Film Synthesis Compatibility

The proposed five-layer architecture is compatible with established, high-throughput industrial thin-film deposition techniques8.

Physical vapor deposition—including electron-beam evaporation with ion-assisted deposition (IAD) and radio-frequency (RF) or direct-current (DC) reactive magnetron sputtering—allows sequential deposition of , and  within a single vacuum chamber cycle9. Sputtering from metallic silicon, aluminum, and silver targets in reactive argon/oxygen and argon/nitrogen atmospheres yields dense, stoichiometric films with precise thickness control below 7.

Alternatively, atomic layer deposition (ALD) can be employed for the  and  layers using trimethylaluminum (TMA) and silane-based precursors, providing conformal, pinhole-free coatings on large-area or curved surfaces8.

By eliminating scarce hafnium precursors and avoiding the near-UV photo-catalytic degradation characteristic of , this earth-abundant five-layer stack provides an economically viable, mechanically durable path toward scalable daytime radiative cooling2.

## Conclusions

The five-layer metal-dielectric photonic coating developed herein demonstrates that high-performance passive daytime radiative cooling can be achieved using earth-abundant materials while reducing structural complexity relative to established benchmarks3.

By sequentially integrating  (),  (),  (),  (), and  () on an opaque silver substrate, the design satisfies all operational constraints, restricting individual layer thicknesses between  and  and maintaining a sub-micron cumulative thickness of 8.

Excluding  eliminates near-ultraviolet interband absorption, enabling the stack to achieve an integrated solar reflectance of  across the  spectrum2.

In the mid-infrared, the multi-component Reststrahlen lattice vibrations of , , and , outcoupled through the top  admittance-matching layer, yield an average atmospheric window emissivity of 7.

Under direct AM1.5 midday solar irradiation () at ambient thermal equilibrium (), the coating delivers a net radiative cooling power of , exceeding the target performance threshold of  and outperforming the landmark Stanford seven-layer  benchmark ()3.

Furthermore, using  as the bottom dielectric layer buffers thermal expansion mismatch and protects the silver substrate from environmental degradation7.

This combination of optical selectivity, thermal performance, and mechanical reliability establishes a practical framework for zero-energy thermal management in building envelopes, solar energy infrastructure, and outdoor electronic systems1.

#### Works cited

- Effective Properties of Semitransparent Radiative Cooling Materials, https://www.osti.gov/servlets/purl/1880322

- Metamaterial-Based Radiative Cooling: Towards Energy-Free All, https://oasis.postech.ac.kr/bitstream/2014.oak/94918/1/energies-12-00089.pdf

- Passive radiative cooling below ambient air temperature under, https://web.stanford.edu/group/fan/publication/Raman_Nature_515_540_2014.pdf

- Radiative Cooling: Principles, Progress, and Potentials - PMC - NIH, https://pmc.ncbi.nlm.nih.gov/articles/PMC5067572/

- Radiative sky cooling: Fundamental principles, materials, and, https://pubs.aip.org/aip/apr/article/6/2/021306/570227/Radiative-sky-cooling-Fundamental-principles

- 2021 - Nano Energy. Review of Radiative Cooling Materials ... - Scribd, https://www.scribd.com/document/1045135414/2021-Nano-Energy-Review-of-Radiative-Cooling-Materials-Performance-Evaluation-and-Design-Approaches

- Supporting Information - ACS Publications, https://pubs.acs.org/aaemcq/article-supplement/5078313/pdf/ae6c00716_si_001/

- Thermostable 1D Photonic Multilayer with Si 3 N 4 - ACS Publications, https://pubs.acs.org/aaoma6/article/4/3/816/5086886/Thermostable-1D-Photonic-Multilayer-with-Si3N4

- Cost-Effective Inorganic Multilayer Film for High-Performance ... - PMC, https://pmc.ncbi.nlm.nih.gov/articles/PMC12028864/

- Emissivity Prediction of Multilayer Film Radiators by Machine, https://www.espublisher.com/uploads/article_pdf/esee8c790.pdf

- A foundation model for inverse design in optical multilayer thin film, https://www.researching.cn/ArticlePdf/m00091/2024/7/7/240062.pdf

- Deep-learning-based multilayer nano-film structure reverse design, https://www.researching.cn/ArticlePdf/m00005/2026/24/4/042201.pdf

- Optical EnginEEring + applicatiOns nanOsciEncE + ... - SPIE, https://spie.org/documents/ConferencesExhibitions/Programs/Archived%20Programs2/OP14-Abstracts%20lr.pdf

- Performance simulation of polymer‑based nanoparticle and void, https://d-nb.info/1226641296/34

- unknown_url

- Deep-learning-based multilayer nano-film structure reverse design, https://opg.optica.org/col/abstract.cfm?uri=col-24-4-042201

- Spectrally Selective Nanoparticle Mixture Coating for Passive, https://pure.korea.ac.kr/en/publications/spectrally-selective-nanoparticle-mixture-coating-for-passive-day/

- Recent Advances in Spectrally Selective Daytime Radiative Cooling, https://d-nb.info/1372058982/34

- The reaction pathway involved in sol-gel synthesis of metal oxide, https://www.researchgate.net/figure/The-reaction-pathway-involved-in-sol-gel-synthesis-of-metal-oxide-nanostructures_fig8_341556138

- UCLA Electronic Theses and Dissertations - eScholarship.org, https://escholarship.org/content/qt1d88x3gf/qt1d88x3gf.pdf

- Photonic structures in radiative cooling - PMC - NIH, https://pmc.ncbi.nlm.nih.gov/articles/PMC10235094/

- Passive isothermal film with self-switchable radiative cooling-driven, https://pmc.ncbi.nlm.nih.gov/articles/PMC11392948/

- Robust Radiative Cooling in Functionalizable Silica Microsphere, https://arxiv.org/html/2606.00565v1

- Progress on Natural and Sustainable Materials for Daytime, https://pubs.acs.org/aaoma6/article/2/6/945/444569/Progress-on-Natural-and-Sustainable-Materials-for